## Slide 1: SYNTHESIS & CHARACTERIZATION OF PORPHYRIN-FULLERENE DYADS FOR APPLICATION IN DYE – SENSITIZED SOLAR CELL (DSSCs)
MAVIS FORSON
(GRADUATE STUDENT; UNIVERSITY OF ARKANSAS AT LITTLE ROCK)

## Slide 2: INTRODUCTION

## Slide 3: SYNTHESIS OF DYADS
Dyad 1
Dyad 2
Zn-Dyad 1
Zn-Dyad 2
Synthesis of dyads was confirmed with
NMR
Mass Spectrometer
FT-IR

## Slide 4: Photophysical Characterization

## Slide 5: Photophysical Characterization
 | λmax (nm) | ε (Lmol-1cm-1) | ΦF
Dyad 1 | 422 518 | 3.71 x 105 1.20 x 103 | 12.37
Zn-Dyad 1 | 430 560 | 4.86 x 105 1.50 x 104 | 2.46
Dyad 2 | 422 517 | 3.69 x 105 1.80 x 104 | 17.45
Zn-Dyad 2 | 430 560 | 4.73 x 105 1.80 x 104 | 1.25
 | τ1 (ns) | α1 | τ2 (ns) | α2 | χ2
Dyad 1 | 1.52 | 0.9293 | 4.35 | 0.0707 | 1.65
Zn-Dyad 1 | 0.359 | 0.9657 | 5.26 | 0.0343 | 1.42
Dyad 2 | 2.10 | 0.9345 | 6.56 | 0.0655 | 1.51
Zn-Dyad 2 | 0.253 | 0.9444 | 4.42 | 0.0556 | 1.59
Table 2. Fluorescence lifetimes recorded at 390 nm excitation/650 nm emission in Benzonitrile.
Table 1. Molar Absorptivity and Fluorescence quantum yield of dyads in Benzonitrile.

## Slide 6
Future Work:
Perform photoelectrical studies for device fabrication.
Acknowledgements:
Dr. Brain Berry and Dr. Noureen Siraj
Ashley Anderson
Samantha Macchi
Dr. Siraj’s Research Group
UA Little Rock Chemistry Department
References
(1) Peng, H.-Q.; Niu, L.-Y.; Chen, Y.-Z.; Wu, L.-Z.; Tung, C.-H.; Yang, Q.-Z. Chem. Rev. 2015, 115, 7502.
(2) Chung, C.-L.; Chen, C.-H.; Tsai, C.-H.; Wong, K.-T. Org. Electron. 2015, 18, 8.
(3) Imahori, H.; Tkachenko, N. V; Vehmanen, V.; Tamaki, K.; Lemmetyinen, H.; Sakata, Y.; Fukuzumi, S. J. Phys. Chem. A. 2001, 105, 1750.
Conclusion:
We successfully synthesized two dyads with different bridge chain and their Zn metallated versions.
Photophysical characterization shows promising results.